## Slide 1: Simple Powder X-ray Diffraction Analysis Pattern matching for phase purity
Rebecca Ricciardo, The Ohio State University
ricciardo.10@osu.edu
Created by Rebecca A Ricciardo, The Ohio State University (ricciardo.10@osu.edu) and posted on VIPEr (www.ionicviper.org) on June 30, 2013. Copyright Rebecca A Ricciardo 2013. This work is licensed under the Creative Commons Attribution-NonCommerical-ShareAlike 3.0 Unported License. To view a copy of this license visit http://creativecommons.org/about/license/

## Slide 2: Solid State Synthesis
Micron Sized Powders
(Starting Materials)
Grind
Heat
Re-grind & Heat again
SrCO3(s) + MoO3(s)  SrMoO4(s) + CO2 (g)

## Slide 3: Solid State Synthesis Calculation
How many grams of each reactant will be needed to synthesize 2.00 g of SrMoO4 from SrCO3 and MoO3?
SrCO3(s) + MoO3(s)  SrMoO4(s) + CO2 (g)
The sample is heated in a crucible for 4 hours at 500 °C
How do we know what we made?
2.00 g SrMoO4 1 mol SrMoO4 1 mol SrCO3 147.63 g SrCO3 1.193 g SrCO3
247.56 g SrMoO4 1 mol SrMoO4 1 mol SrCO3
×
×
×
=
2.00 g SrMoO4 1 mol SrMoO4 1 mol MoO3 143.94 g MoO3 1.163 g MoO3
247.56 g SrMoO4 1 mol SrMoO4 1 mol MoO3
×
×
×
=

## Slide 4: There are many peaks, and we need to account for all of them!!
SrCO3(s) + MoO3(s)  SrMoO4(s) + CO2 (g)

## Slide 5: SrMoO4 is present, but there are still peaks unaccounted for.
We can match the pattern to a data base of known XRD patterns and see what we find
SrCO3(s) + MoO3(s)  SrMoO4(s) + CO2 (g)

## Slide 6: SrCO3 is also present, but there are still peaks unaccounted for.
SrCO3(s) + MoO3(s)  SrMoO4(s) + CO2 (g)

## Slide 7: We have some product, but also some reactants that are unreacted “impurities”
Let’s grind and reheat the sample for 4 hours at 700 °C
MoO3 is also present, and now all of the peaks are accounted for

## Slide 9: SrMoO4 is present, and all of the peaks are accounted for. We can say the product is PURE