## Slide 1: Six Slides about Polypropylene Stereochemistry and Identification by 13C NMR Spectroscopy
Shirley Lin
Department of Chemistry
United States Naval Academy
Created by Shirley Lin, United States Naval Academy. Posted on www.ionicviper.org on July 17, 2012.
Copyright Shirley Lin 2012. This work is licensed under the Creative Commons Attribution Non-commercial Share Alike License. To view a copy of this license visit http://creativecommons.org/licenses/by-nc-sa/3.0/

## Slide 2: Stereochemistry of Polypropylene
atactic – pendant methyl groups are randomly arranged along polymer backbone
syndiotactic – pendant methyl groups alternate sides of the polymer backbone
isotactic – pendant methyl groups are on the same side of the polymer backbone

## Slide 3: Stereochemistry Determines Properties
Relative stereochemistry of methyl groups in polypropylene
determines polymer properties
atactic - amorphous
syndiotactic - crystalline
isotactic - crystalline
Stereoregular arrangements of methyl groups produce crystalline polymer
Stereorandom arrangements of methyl group produce amorphous polymer

## Slide 4: 13C NMR Reveals Polymer Stereochemistry
m = meso (syn) r = racemo (anti)
On a high field NMR instrument, the chemical shift of the methyl groups on the polymer backbone is sensitive to the relative stereochemistry of its four nearest neighbors (two on each side).

## Slide 5: 13C NMR Spectra of Various Polypropylenes

## Slide 6: Elastomeric Polypropylene
• soft amorphous segments give flexibility
• crystalline segments provides crosslinking
Challenge: What would the 13C NMR spectrum of the methyl region
of this polymer would look like?
Stereoblock structure can account for elastomeric properties;
isotactic segments can co-crystallize, atactic segments are amorphous

## Slide 7: 13C NMR of Isotactic-Atactic Stereoblock Polypropylene
All 10 pentads are observed but the [mmmm] pentad resonance is noticeably increased from what is observed for atactic PP (~ 5%)